## Slide 1: Recent Developments in 2-micron Sources
Peter F. Moulton
MIT Lincoln Laboratory
Working Group on Space-based Lidar Winds
February 7-9, 2018
Boulder, CO
*This material is based upon work supported under Air Force Contract No. FA8721-05-C-0002 and/or FA8702-15-D-0001. Any opinions, findings, conclusions or recommendations expressed in this material are those of the author(s) and do not necessarily reflect the views of the U.S. Air Force. © 2016 Massachusetts Institute of Technology. Delivered to the U.S. Government with Unlimited Rights, as defined in DFARS Part 252.227-7013 or 7014 (Feb 2014). Notwithstanding any copyright notice, U.S. Government rights in this work are defined by DFARS 252.227-7013 or DFARS 252.227-7014 as detailed above. Use of this work other than as specifically authorized by the U.S. Government may violate any copyrights that exist in this work.

## Slide 2: Approaches to diode-pumping of Ho-doped lasers
A. Dergachev, P. F. Moulton, and T. E. Drake, “High-power, high-energy, high-repetition-rate 2050-nm Ho:YLF laser,” SPIE Photonics West, 2005

## Slide 3: Approaches to diode-pumping of Ho-doped lasers
A. Dergachev, P. F. Moulton, and T. E. Drake, “High-power, high-energy, high-repetition-rate 2050-nm Ho:YLF laser,” SPIE Photonics West, 2005

## Slide 4: 2:1 pumping enables efficient Tm-doped lasers, including silica-based fibers
S. D. Jackson, A. Sabella, and D. G. Lancaster, “Application and development of high-power and highly efficient silica-based fiber lasers operating at 2 μm,” IEEE J. Sel. Top. Quantum Electron. 13(3), 567–572 (2007).

## Slide 5: All-glass, efficient Tm:fiber (silica) laser
Ehrenreich, T., Leveille, R., Majid, I., Tankala, K., Rines, G. & Moulton, P. 1-kW, all-glass Tm: fiber laser. Fiber Lasers VII: Technology, Systems, and Applications, San Francisco, California, USA. Proceedings of SPIE (International Society for Optics and Photonics). (2010, January 23).

## Slide 6: Results from all-glass system
Ehrenreich, T., Leveille, R., Majid, I., Tankala, K., Rines, G. & Moulton, P. 1-kW, all-glass Tm: fiber laser. Fiber Lasers VII: Technology, Systems, and Applications, San Francisco, California, USA. Proceedings of SPIE (International Society for Optics and Photonics). (2010, January 23).

## Slide 7: Two-stage power amplifier provides power scaling
Ehrenreich, T., Leveille, R., Majid, I., Tankala, K., Rines, G. & Moulton, P. 1-kW, all-glass Tm: fiber laser. Fiber Lasers VII: Technology, Systems, and Applications, San Francisco, California, USA. Proceedings of SPIE (International Society for Optics and Photonics). (2010, January 23).

## Slide 8: Result: > 1kW of power output at 2045 nm
Ehrenreich, T., Leveille, R., Majid, I., Tankala, K., Rines, G. & Moulton, P. 1-kW, all-glass Tm: fiber laser. Fiber Lasers VII: Technology, Systems, and Applications, San Francisco, California, USA. Proceedings of SPIE (International Society for Optics and Photonics). (2010, January 23).

## Slide 9: Tm:fibers (silica) still undergoing development

## Slide 10: Approaches to diode-pumping of Ho-doped lasers
A. Dergachev, P. F. Moulton, and T. E. Drake, “High-power, high-energy, high-repetition-rate 2050-nm Ho:YLF laser,” SPIE Photonics West, 2005
Which Ho-laser?

## Slide 11: Ho:YLF vs. Ho:YAG
Ho:YLF
  Higher emission cross-section
  Long upper laser level lifetime ~ 15 ms
  Naturally birefringent material
  Low dn/dT –> weak thermal lensing
  ~5% quantum defect
Ho:YAG
  Excellent thermo-mechanical properties
  Upper state lifetime 7 ms
  Isotropic
  Strong thermal lensing
  ~10% quantum defect
A. Dergachev, P. F. Moulton, and T. E. Drake, "High-power, high-energy Ho:YLF laser pumped with Tm:fiber laser," in Advanced Solid-State Photonics (TOPS), C. Denman and I. Sorokina, eds., Vol. 98 of OSA Trends in Optics and Photonics (Optical Society of America, 2005), paper 608.

## Slide 12: Ho:YLF laser designs with Tm:fiber pump
Osc/Amp module
Dual-crystal amplifier module
~50 mJ, ~20 ns
up to 500 Hz
+ ~50 mJ
up to 500 Hz
Alex Dergachev, Darrell Armstrong, Arlee Smith, Thomas Drake, Marc Dubois, "High-power, high-energy ZGP OPA pumped by a 2.05-μm Ho:YLF MOPA system", Proc. SPIE 6875, Nonlinear Frequency Generation and Conversion: Materials, Devices, and Applications VII, 687507 (13 February 2008)

## Slide 13: Performance of Osc/Amp module
Alex Dergachev, Darrell Armstrong, Arlee Smith, Thomas Drake, Marc Dubois, "High-power, high-energy ZGP OPA pumped by a 2.05-μm Ho:YLF MOPA system", Proc. SPIE 6875, Nonlinear Frequency Generation and Conversion: Materials, Devices, and Applications VII, 687507 (13 February 2008)

## Slide 14: Three-stage system: 115 W cw or 170 mJ pulses
Alex Dergachev, Darrell Armstrong, Arlee Smith, Thomas Drake, Marc Dubois, "High-power, high-energy ZGP OPA pumped by a 2.05-μm Ho:YLF MOPA system", Proc. SPIE 6875, Nonlinear Frequency Generation and Conversion: Materials, Devices, and Applications VII, 687507 (13 February 2008)
Ho-stage/ Regime | CW | 100 Hz | 500 Hz
Osc/Amp #1 | 39 W | 55 mJ | 50 mJ
Amp#2 | 76 W | 110 mJ | 95 mJ
Amp#3 | 115 W | 170 mJ | 140 mJ
Tm-pump #1
~120 W at 1940 nm
Osc/
Amp #1
Amp #2
Amp #3
Tm-pump #2
~120 W at 1940 nm
Tm-pump #3
~120 W at 1940 nm
Tm-fiber laser TLR-100-1940
IPG Photonics
www.ipgphotonics.com
Operation regime | CW
Beam Profile | TEMoo
Output power | ≥ 120 W
Wavelength | 1940 nm
Polarization | Random
Linewidth | ≤ 2 nm

## Slide 15: 45-dB gain Ho:YLF amplifier
A. Dergachev, "45-dB, Compact, Single-Frequency, 2-µm Amplifier," in Lasers, Sources, and Related Photonic Devices, OSA Technical Digest (CD) (Optical Society of America, 2012), paper FTh4A.2.

## Slide 16: Newer work: Ho:YLF oscillator scaled to 550 mJ
Helge Fonnum, Espen Lippert, and Magnus W. Haakestad, "550 mJ Q-switched cryogenic Ho:YLF oscillator pumped with a 100 W Tm:fiber laser," Opt. Lett. 38, 1884-1886 (2013)

## Slide 17: Conclusions
There are several technical approaches to the construction of high-energy, Ho-doped, 2-micron lasers suited for wind-sensing applications
Advances is silica-based, Tm-doped fibers have led to demonstration of high-efficiency devices with > 1 kW of cw output power
This has enabled one technology approach, Tm:fiber-pumped Ho-doped lasers, to reach performance levels commensurate with requirements for space-based wind sensors
All of the components of a system, including high-gain amplifiers and high-energy amplifiers, have been developed based on 2050-nm, Ho:YLF bulk crystals pumped by 790-nm-diode-pumped Tm:silica fibers
The technology approach looks well-positioned for engineering into space-based hardware, featuring:
  CW, fiber-coupled diode pump lasers, which can be remotely located and conduction cooled
  Fiber-delivered pump power to high-energy amplifiers
  Efficient, low-thermal-load/distortion, bulk crystals for high-energy pulse generation